SYNTHESIS AND CHARACTERIZATION OF NANOSTRUCTURED SILVER BASED ANTIBACTERIAL COATINGS ON PROTECTIVE POLYMER FOILS OF TOUCH SCREEN DEVICES

# Catalin VITELARU1, Anca C. PARAU1, Adrian E. KISS1, Iulian PANA1, Mihaela DINU1, Lidia R. CONSTANTIN1, Alina VLADESCU1,2, Lavinia E. TONOFREI3, Cristina S. ADOCHITE4, Sarah COSTINAS4, Liliana ROGOZEA4, Marius MOGA4, Mihaela E. IDOMIR4, Mihaela BADEA4

## 1- National Institute for Research and Development in Optoelectronics INOE 2000, Magurele, Romania;

## 2- Research Center for Physical Materials Science and Composite Materials, Research School of Chemistry &Applied Biomedical Sciences, Tomsk Polytechnic University, Tomsk, Russia

3- ATS Novus SRL, Bucharest, Romania

4- Faculty of Medicine, Transylvania University of Brasov, Brasov, Romania

## catalin.vitelaru@inoe.ro

The use of electronic devices that are frequently touched can contribute to the spread of various pathogens, leading to bacterial and fungal infections. In this study we investigate the use of very thin layers of silver nanoparticles embedded into a dielectric layer, as antimicrobial thin films on the surface of self-adhesive polymer covers for touch screen devices. Physical vapor deposition technique was used, combining High-Power Impulse Magnetron Sputtering (HiPIMS) for the deposition of Ag nanoparticles with Radio Frequency (RF) sputtering for the deposition of oxides. The characterization of the coatings incudes: elemental and phase composition, texture, structure, topography of the coatings, evaluation of optical properties. The antimicrobial activity of the foils was assessed, using E-coli bacteria at different concentrations. Thin films in the range of ~30 nm thickness, including Ag as active antimicrobial agent and SiO2 and TiO2 as dielectric matrices, were obtained and characterized. Good transparency in the visible spectral range was proven along with good responsiveness to touch. The presence of nanostructured Ag was demonstrated also by spectrophotometric measurements and XRD measurements, indicating the presence of ~10nm size nano-grains. Comparisons between different film compositions and antibacterial testing methods is also provided.

Acknowledgments

This work was supported by a grant of the Ministry of Research, Innovation and Digitization, CNCS/CCCDI – UEFISCDI, project number PN-III-P2-2.1-PED-2019-4966 PED 489, within PNCDI III, Core Program, Project no. 18N/2019 and through Program 1- Development of the national research-development system, Subprogram 1.2 - Institutional performance - Projects to finance the excellent RDI, Contract no. 18PFE/30.12.2021.

Keywords: antimicrobial, nanostructured silver, magnetron sputtering